## Slide 1: Mechanical tests on silicon fibers
Michele Arcangelo Dicorato, Flavio Travasso – University of Camerino, University of Perugia, INFN Perugia
Ardiana Nela, Andrew Spencer – IGR, University of Glasgow
Iryna Buchovska, Robert Menzel – Institut für Kristallzüchtung, Berlin
Alex Amato, Maike Kuhler – Maastricht University
Alessandro Bertolini - Nikhef
14 th KAGRA International Workshop, 2026

## Slide 2: Outline
Why crystalline test-mass suspension
Fiber sizing
Fiber production
Fibers mechanical characterization
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026
Q-factor measurement
Tensile strength measurement
Bending strength measurement

## Slide 3
Monocrystalline silicon is one of the most promising candidate materials.
This is due to its thermoelastic nulling regions (zero crossing of the thermal expansion coefficient at 18K and 123K) and low mechanical loss at cryogenic temperatures.
Blade
Ear
Substrate
Marionette
Fiber
Anchor
Heat load
Mirror mass 211 kg
SUSPENSION REQUIREMENTS:
High thermal conductivity
High breaking strength
Low mechanical loss (loss angle )
Low resonant frequency (< 2 Hz)
220 MPa with a safety factor of 3
Low thermal noise
Cryogenic temperature (10 K -20 K )
Excellent surface quality
Towards the development of a silicon cryogenic suspension
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026

## Slide 4
Fiber sizing
Mirror temperature as a function of marionette temperature for some rod diameters, considering 4 silicon rods of length 1,2 m and a heat load of 0,5 W
CURRENT DIAMETER BASELINE CHOICE: 3 mm
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026
Thermal conductivity of silicon taken from Material Properties Database (MPDB) software
Thermal gradient of a rod long 1,2 m with diameter 3 mm for K and heat load 0,5 W

## Slide 5
4 wires of 3 mm diameter
211 kg mirror
Stress on each wire = 73 MPa
Safety factor of 3 or 6
220 MPa or 440 MPa tensile strength
High variability in the breaking strength measurements
Improvement of production process and breaking strength measurements to reduce the safety factor.
BREAKING STRENGTH
LENGTH
A decreasing length yields a reduction of temperature of the mirror, but also shift all the modes to higher frequencies.
Constraint imposed by the tower dimensions and cryostat dimensions
CURRENT REFERENCE LENGTH: 1,2 m
Fiber sizing
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026

## Slide 6
LEIBNIZ - INSTITUT FÜR KRISTALLZÜCHTUNG
Crystal
HF
Inductor
Feed
Melt
Pulling
Pulling
Pedestal growth
Float zone growth
Float-zone technique produces high purity, contaminant free, single crystal uniform silicon fibers with exceptionally good surface quality.
A silicon feed rod is melted at the bottom using an inductive coil
The molten zone contacts a monocrystalline seed
The seed is moved downwards, and crystallization begins
Molten silicon solidifies into a large single crystal silicon fiber without direct contact with seed rod, minimizing impurities
Fiber production
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026

## Slide 7
Long fibers with grown thicker ends
Welding of 3 mm rods
Welding of 8 mm rods
Fiber production
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026

## Slide 8
Mechanical loss measurements
Mechanical loss measurements at the University of Camerino to accurately measure the loss of fibers with the ring-down method
Clamp material (rigidity, density)
Clamp dimensions
Fastening strength
If the fiber has an excellent surface quality and a good crystallinity, the limiting factor for this measurement at cryogenic temperature is the clamp loss
[Douglas M. Photiadis and John A. Judge Attachment losses of high Q oscillators]
Fiber characterization
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026

## Slide 9
[Douglas M. Photiadis and John A. Judge Attachment losses of high Q oscillators]
Fiber characterization
Attachment loss estimation – clamp sizing
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026
Silicon fiber
Diameter 3 mm
Length 10 cm
Clamp
Thickness 18 cm
Temperature 15 K

## Slide 10
Tensile stress measurements
Vertical Alignment with micrometric controls and laser level
Fiber with seed
(Perugia method)
Fiber without seed
(Glasgow method)
Work done with Ardiana Nela and Dr Flavio Travasso at the University of Perugia
Fiber characterization
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026

## Slide 11
Bending system designed and optimized for cylindrical rods 3 mm thick and 5 cm long, according to the standard ASTM C1684-18 2023
[Quinn et al., Journal of Testing and Evaluation, 2009]
2a
4-point bending method
Work done with Ardiana Nela and Dr Flavio Travasso at the University of Perugia
Why bending test?
To determine the assembly precision (some misalignment in the assembly can cause the fiber to bend)
To determine the dynamic displacement range during the setup of the active controls
Maximum tensile stress
Fiber characterization
Bending stress measurements
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026

## Slide 12
Lloyd LD50 testing machine with 5kN load cell (set to apply a uniform displacement of 5 mm/min)
Ultra high speed camera (set to 5000 fps)
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026
Fiber characterization
Bending stress measurements - setup

## Slide 13
Data dispersion on tensile tests is most likely due to imperfection on the fibers (microcracks): maybe not optimal shipping and handling technique
The good news is that fibers don’t break at the welding point
Tensile tests
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026
Expected value

## Slide 14
Lower dispersion but still some outliers
From the high speed camera we can see that the break is probably due to a microcrack on the surface of the fiber
Bending tests
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026
Stress [MPa]

## Slide 15
GOOD SAMPLE
OUTLIER
Bending tests
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026

## Slide 16
Handling – alignment comparison
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026

## Slide 17
Summary
A big international effort is being put into research and development of suspension components for ET-LF
The float zone has been proven to be a very reliable production technique for silicon fibers
A new clamping system is under study to accurately measure the Q-factor of silicon fibers
In tensile tests alignment and shipping/handling techniques are crucial to accurately measure breaking strength of fibers
Production techniques of fibers must be improved to increase the reliability and standardize the entire process from production to the mounting
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026

## Slide 18: Thank you 
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026

## Slide 19: Supplementary slides
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026

## Slide 20
Tensile strength depends on:
Crystalline structure
Production method
Surface quality (every scratch is a possible point of stress accumulation and thus breakage)
Soft plastic box
Metal tubes with rings and wax
Packaging
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026

## Slide 21
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026

## Slide 22
Measuring mechanical dissipation means evaluating the thermal noise of a system (Fluctuation-dissipation theorem)
The loss-angle quantifies the mechanical dissipations of an oscillator
Transfer function
FDT
Thermal noise power spectral density
Resonant peak
if
Perturbed oscillator with mechanical dissipations
Loss-angle
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026

## Slide 23
The energy stored in gravity is lossless and dominates in heavily loaded suspension fibers. This implies that the pendulum loss is lower than that of the material used for the suspension fiber: the only mechanical loss in each cycle is of the total energy stored in the oscillating rod.
n: number of wires
E: Young’s modulus
T: tension of the wire
In the high frequency limit
Pendulum thermal noise goes like
And also like
Why large and heavy mirrors?
To keep the radiation pressure effect low
To allow large-sized beam spots on the mirror surfaces for lowering thermal noise
Dilution factor
Losses in a pendulum
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026

## Slide 24
Bulk loss-angle at 10 K:
Silicon <100>
4 wires
Length: 1,2 m
Diameter: 3 mm
Mirror mass: 211 kg
Average temperature: 15 K
Pendulum mode
First violin mode
Suspension thermal noise (STN)
  Michele Arcangelo Dicorato, Mechanical tests on silicon fibers, KAGRA International Workshop 2026