## Slide 1: Birefringence measurement and mitigation techniques
Frederic Cleva, Marc Eisenmann, Stephanie Grabielle, Clement Jacquet, Shalika Singh, Haoyu Wang, Chenjie Zhou

## Slide 2: KAGRA and crystalline test-masses
KAGRA operates with Sapphire test-masses at cryogenic temperature
Sapphire test-masses
23 kg
22 cm diameter
15 cm thickness
Optical axis along c-axis

## Slide 3: Sapphire and birefringence
Perfect sapphire along c-axis should be birefringence free
Manufacturing defects, stress, or optical axis fluctuations can generate birefringence

## Slide 4: KAGRA and birefringence
The non-uniform birefringence of KAGRA test-masses generates several noises, increase optical losses and spoil controls

## Slide 5: Birefringence studies in optical cavity
Birefringence
Birefringence can affect optical cavity control
Custom waveplate
Carrier
Control
Sideband
Misalignment

## Slide 6: The compensation strategy
Birefringent input test-mass
Birefringent input test-mass
Birefringence compensation system
The birefringence compensation system generates the opposite polarization than the one generated by the test-mass

## Slide 7: Variable polarization retarder
Each pixel of a Liquid Crystal Display (LCD) contains a liquid crystal
Liquid crystals are birefringent molecules that align with the electric field
Light source
Polarizer
Liquid crystal
Polarizer

## Slide 8: Variable polarization retarder
Each pixel of a Liquid Crystal Display (LCD) contains a liquid crystal
Non-uniform in transverse plane : high retardation
Uniform in transverse plane : low retardation
Liquid crystals are variable polarization retarders
Retardation[nm]

## Slide 9: Full polarization control
Using a pair of liquid crystals (variable polarization retarders) with their axis separated by 45o it is possible to generate any polarization
The 1st liquid crystal acts on polarization rotation
The 2nd liquid crystal acts on polarization retardation

## Slide 10: 1D birefringence compensation
https://doi.org/10.1364/OL.523753
Achieved a reduction of birefringence by a factor 105 in 1 position

## Slide 11: Birefringence measurement
Birefringent input test-mass
Use variable retarders to generate arbitrary polarization
Probe the Jones matrix (J) of the sample
Extract birefringence from the Jones matrix
Works for transmissive or reflective components
https://doi.org/10.1364/OE.558774

## Slide 12: 2D variable retarders
Spatial ligh modulator contains ~ 1 Mpixels
Each half of SLM acts as a variable retarder

## Slide 13: 2D polarization control

## Slide 14: Fast polarization control
Liquid crystals are usually slow (~100 Hz)
Using crystals (eg Pockels cell) can go to MHz
Allows for higher statistics, probe time-dependent birefringence, and study impact on control sidebands

## Slide 15: Birefringence compensation in KAGRA
Require stable CO2 laser power (typically 20% fluctuations out of the box)

## Slide 16: Low loss variable retarder
Liquid crystal, electro-optic modulator, spatial light modulator etc… have too large optical losses and too low power tolerance to be installed inside KAGRA (at least for the main laser beam)
We are now developing low-loss non-uniform polarization control
CO2 laser

## Slide 17: CO2 laser power stabilization

## Slide 18: Conclusion
Birefringence of crystalline test-masses can limit GW detectors sensitivity
We are now tackling birefringence issues from several angles
  New birefringence measurement technique
  Static birefringence compensation
  Dynamic birefringence compensation
We aim for low-loss compensation of non-uniform birefringence in KAGRA