## Slide 1: Materials for ET-LF Core optics and Suspensions
ISB workshop October 2022 – Parallel session 1
A. Amato

## Slide 2
Core Optics – Tasks for Workshop
Core Optics - ISB workshop October 2022
Parameters
Define better estimate about substrate production (diameter, absorption, …)
Define the missing data for R&D (both substrate and coatings)
AlGaAs: time and costs – Is it a real option?
Heat Extraction
Absorbed power with measured absorption
Safety factor = 6 -> “fibre” size?
Fibres TN, Bounce frequencies, …?

## Slide 3
Summary
PARAMETERS:
We need to keep record of the evolution of the parameters + desired parameters
A new database will be created.
Materials Parallel Session 1 - ISB workshop October 2022
DRAFT

## Slide 4
Suspension – Jointing and Strength
Core Optics - ISB workshop October 2022
Jointing methods dominant noise source
  Require ability to lower joint loss and/or shape silicon to drive energy from lossy joint regions crucial to design
  ≈1 millionth energy in all bonds for joints to match next dominant loss mechanism (surface)
  Accurate, representative modelling required to determine joint thermal noise contribution
1.2 m length confirmed between cryogenics and suspensions group
  Some techniques compatible with this length but work required to demonstrate this in practice
  Caution: Increasing stress may being vertical/bounce mode <30 Hz
Safety factor of 6 decided with current reference stress at 120 MPa for silicon
  More work required to strengthen silicon/reduce SF, without increasing surface loss
  Caution: current surface loss value (1e-9 is best measured value – not necessarily representative of real ribbon/fibre)

## Slide 5
Suspension – Heat Extraction and STN (and errata!)
Core Optics - ISB workshop October 2022
  Old values κcurve 19 = 6300 W/m.K κcurve 27 = 37000 W/m.K
  Corrected values κcurve 19 = 400 W/m.K κcurve 27 = 2300 W/m.K (mean value used by A. Amato ≈1300 W/m.K)
  Decided suspension TN calculations based on 0.5 W heat load
  Suspension TN calculations correct but incorrect conductivities used for model 19 and 27
  Forgot to divide integrated κ over PUM-TM temperature range giving artificially high κ

## Slide 6
Suspension – Heat Extraction and STN (and errata!)
Core Optics - ISB workshop October 2022
Scenario | Fibre radius, r (μm) | Ribbon thickness (5:1 ratio), t (μm) | Stress (MPa) | Safety factor
Medium power (550 mW) – curve 19 “Low κ” | 1312 / 5750 | 1040 / 4558 | 91 / 4.7 | 1.3  / 25 
Medium power (550 mW) – curve 27 “High κ” | 1976 / 2382 | 1566 / 1888 | 40 / 27.5 | 3  / 4.4 
Strength limited (Safety factor = 3) | 1976 | 1566 | 40 | 3 
Strength limited (Safety factor = 6) | 2794 | 2215 | 20 | 6 
 | Old incorrect value | Reference | 120 | 6 (aLIGO/AdV)
  This slightly modifies the conclusions presented in my plenary

## Slide 7
Summary
Materials Parallel Session 1 - ISB workshop October 2022
Fibers Size
Thermal Resistance
Thermal Cond.
Fiber Length
Fiber Surface
4 K
20 K
Bending distance and Dilution Factor
Safety Factor from T
Breaking strength
BS = 120 MPa
(averaged integrated value)
Simplified STN
With

## Slide 8
Heat dominated for Touloukian’s curve 19 (“low κ” case)
Strength dominated (SF 6) for Touloukian’s curve 27 (“high κ” case)
Same caveats as before: Suspension thermal noise only No jointing loss included
Total ET-D noise
Priority: experimentally measure and verify conductivity of real silicon ribbons
Caution: higher κ means strength must improve (and must not forget boundary scattering for high κ)