## Slide 1: Cryogenic measurements of the loss angle of thin films: a geometric approach
Alex Amato, Gianpietro Cagnoli, Federica Fabrizi, Massimo Granata, Matteo Montani, Lorenzo Mereni, Francesco Piergiovanni, Laura Silenzi, Angela Trapananti, Flavio Travasso

## Slide 2: Why cryogenic measurement
To obtain information on the processes that produce the mechanical losses
…e.g., fused silica measurements
Loss angle vs Temperature => info on the Asymmetric Double Well Potential (ADWP) that rules this process at low temperature
VIR-1070A-22
EPL, 80 (2007) 50008, doi: 10.1209/0295-5075/80/50008
Loss angle vs Frequency at different temperature

## Slide 3: Why silicon and sapphire
HV
Materials that have excellent thermal conduction characteristics and a high-quality factor at low temperatures
A geometry that allows the measurement of many resonance frequencies
Cheap to have a good statistics
The first idea was to use the materials proposed for ET (silicon and sapphire) and to use them for the study of the coatings
+
Second meas.
First meas.
Extrapolation
+
Cesarini E. & al, Rev. Sci. Instrum. 80 (2009)
M. Granata et al. VIR-0499A-16

## Slide 4: Thermoelastic losses
Thermoelastic losses happen when a body is bent => one side gets compressed (heated) and the other gets expanded (cooled). Heat flows from a side to the other.
No bending in pure expansion =>
=> there are no thermoelastic losses
Set the amplitude => strong dependency with α => for silicon, α = 0 for 2 temp. (120K, 18K)
Time of thermal diffusivity => to compare with period of oscillations => maximum TE when they are equal
Thermoelastic peak vs. thickness
Thermoelastic peak vs. temperature

## Slide 5: ...a geometrical approach
Chart: ϕ_TE
First family | 0.00053559 | 0.00053559 | 0.00053559 | 0.00053559 | 0.00053559 | 0.00053559 | 0.00053559 | 0.00053559 | 0.00053559 | 0.00053559 | 0.00053559 | 0.00053559 | 0.00053559 | 0.00053559 | 0.00053559 | 0.00053559 | 0.00053559
Second Family | 0.00056109 | 0.00056109 | 0.00056109 | 0.00056109 | 0.00056109 | 0.00056109 | 0.00056109 | 0.00056109 | 0.00056109 | 0.00056109 | 0.00056109 | 0.00056109
Third Family | 0.0005866 | 0.0005866 | 0.0005866 | 0.0005866 | 0.0005866 | 0.0005866 | 0.0005866 | 0.0005866 | 0.0005866
Forth Family | 0.0006121 | 0.0006121 | 0.0006121 | 0.0006121 | 0.0006121 | 0.0006121
Phi_Dil - First Family | 4.4347e-06 | 1.7034e-05 | 3.2036e-05 | 4.9055e-05 | 6.1969e-05 | 6.834e-05 | 7.1844e-05
Phi_Dil -Second Family | 0.00010272 | 0.00010835 | 0.00011054 | 9.3144e-05
Phi_Dil - third Family | 0.00011936
RIGHT SIDE OR LEFT SIDE OF TE PEAK??
(see the excel file)
Find a possible "geometric" solution to avoid/reduce the predominance of thermoelastic losses in the frequency region of interest….
...some modes should be not affected by thermoelastic peak, as a function of temperature
Thermoelastic losses for a silicon disk 3 inches in diameter and 0.2 mm thick.
Rev. Sci. Instrum. 77, 044502 (2006), doi: 10.1063/1.2194486
Thermoelastic losses
Resonance frequencies
(modes) of the silicon disk

## Slide 6: Loss angle (work in progress)
Mixed modes
Butterfly modes
Mode (0,2) seems only slightly affected

## Slide 7
Different substrate thickness
Granata M. et al, Archives of Metallurgy and
Materials 60, 2015 DOI: 10.1515/amm-2015-0060
Silicon disk φ=3’’ and th=0.5mm (blue points) vs.
Silicon disk φ=3’’ and th=0.2mm (blue points)
(0,2)
(0,5)
Silicon disk φ=3’’ and th=0.2mm

## Slide 8: Thermoelastic issue: coating
The coated sample represents a composite system (sub + coat) in which the properties of both parts must be considered: thermo-mechanical properties of the coating are usually unknown at any temperature => the thermoelastic peak is unpredictable
F. Fabrizi, VIR-0271A-21
J. E. Bishop and V. K. Kinra, Comp. Mater. Struct. 3 83-95 (1996)
S. Vengallatore et al., Jour. of Micromech. and Microen. (2005)
The difference of the two thermoelastic peaks (substrate only vs. sub+coat) seems to decrease/zero to the left of the peak.

## Slide 9: Next steps and open questions
New geometries are needed for the study of thin films due to bonding (HCB, metal bonding, direct bonding, ….):
asymmetrical approach to avoid bonding in the central part: no energy is stored there => very hard to simulate and to extrapolate the mechanical losses
access to many resonance modes to determine any trends with frequencies
cheap samples (statistics)
easy to handle

## Slide 10: Conclusions
The geometrical approach was able to reduce the effect of thermoelastic => silicon disks of 3inchs-0.2mm can be a good candidate for the study of amorphous coating
Geometrical approach can work, but further tests needed (e.g. increasing the statistics and the sampled temperature points)
Tests with amorphous coating deposition should be done
New geometries are needed for the study of thin films due to bonding