## Slide 1
MIR Sub-System
Coatings fot O5
Update on Ti-Ge coating working group
¶
L. Pinard for the LMA Team

## Slide 2
Coatings for O5
Goal
Deliver a HR stack (T=4-5ppm @1064 nm) with low optical losses and low CTN with Ti-GeO2/SiO2 multilayer
Absorption <1 ppm
Scattering< 10 ppm
CTN reduced by a factor 2 versus Advanced VIRGO coating (Ti-Ta2O5/SiO2)
Uniformity : same as AdV VIRGO/LIGO Test Mass
  Deliverable: HR ETM Stack coated on a pathfinder
  (AdV LiGO Test mass scale 1) in the GC

## Slide 3
Coatings for O5
Status at the end of 2023
  Bubbles after annealing at high T°
  Absorption too high
  CTN best value: 0.8 of aLIGO on HR coated in the GC

## Slide 4
Coatings for O5
Status March 2024
  New Working Point with less Argon (-25%), high T° in the chamber
  Several coating tests of full stack made
    Absorption : :1,2 ppm
    No bubbles after long annealing in the clear aperture (sometimes tiny ones at the edge)
    Scattering # 10ppm
  CTN best value: 0.7 of aLIGO on HR coated in the GC
  Optimization of the annealing cycle : test ongoing.
  To reduce absorption and CTN : optimization of the multilayer design (Sannio)
      Test on going

## Slide 5
Coatings for O5
Next steps
  LIGO: Technical Review Board of the Ti:GeO2 coatings for O5 test masses held end march 2024
  Recommendations :
  “We find the Ti:GeO2 coatings sufficiently developed to proceed with an uniformity test and production, pending successful test”
    “Assuming characteristics found on small optics transfer well to large optics”
    “Use the best optimized design available at the moment, and demonstrated on small scale samples (either TiGeO2/SiO2 or ternary)”
  “Parallel work on improvements should continue during the uniformity test phase”
    “Optimization of annealing schedule to reduce coating thermal noise (CTN), defects (bubbles) and optical absorption”
    “Optimization of coating layer design to reduce CTN and optical absorption (including with ternary coating design with TiO2:Ta2O5)”

## Slide 6
Coatings for O5
Next steps
  To reduce absorption : optimization of the multilayer design (Sannio), 2 Ti-Ta2O5/SiO2 QW doublets added on the top of the (HL)25 H2L stacks
      Goal : absorption #0,5 ppm (theory), CTN improvement 0,7
      Test on going in the coating machine
  If not satisfactory : optimization of TiGeO2/SiO2 stack
  Then : uniformity optimization with a final test on a pathfinder
  Coating of several test masses for LIGO in September 2024