## Slide 1
Available Methods:
Soldering/Brazing
Sintering
Welding
Gluing, etc.
Requirements:
High thermal conductivity
High tensile strength
High Q-factor
Sapphire: Most Promising Technique is Welding
Diffusion Welding
Laser Welding
Constrains:
Specific material properties
Uneven geometry, roughness
Wide temperature working range (10 K – 293 K)
Towards Reliable Bonding of
Sapphire and Silicon

## Slide 2
Processing schema: 1 – melt droplet holder, 2 – melt droplet,
3 – capillary gap, 4 – sapphire parts, 5 – weld seam
Diffusion Welding:
Sapphire Bonding by Its Own Melt
Quasi-stationary solution to the capillary rise
(acceleration neglection):
Taking solidification into account
Heat released during crystallization exceeds the heat released during cooling:
Linear thermal gradient
, - thermal conductivity
Resulting equation for the melt height:
-

## Slide 3
Sapphire Bonding by Its Own Melt:
Technique Improvements
The molybdenum holder for filling capillary channels
Sapphire seeds on the holder before melting
By variation of
Channel Width
Thermal Gradient
The row with capillaries of different width W=0.07..0.450 mm. LxH=5x50 mm.
Bonding optimization by variation of the channel width

## Slide 4
Sapphire-to-Sapphire Ultrashort Pulsed Laser Bonding: Technical Setup
1030 nm near-infrared wavelength
500 fs pulse length, 100 kHz repetition rate
20 – 40 W average power
< 15 µm focal spot size
Multiphoton absorption of USP-Laser gradually heat up the sapphire within a defined volume.
SLM is used for even heat distribution. Adjacent regions remain unaffected.

## Slide 5
Silicon Welding:
Preliminary attempts (2019)
Fragments of the trial to weld a cylindrical rod Ø 0.9, 1.1 mm to a round disk Ø25 x 10 mm. Nd:YAG-laser, wavelength
Attenuation coefficient of silicon in dependence on wavelength
Silicon Welding Outlook: Changing wavelength to =2100 nm
=1064 nm

## Slide 6
Philipp L. Maack, M.Sc.
Jonas Wehner, B.Sc.
Marvin Schuleit, Dr.-Ing.
Aleksander Kostka, Dr.-Ing.
Andreas Ostendorf, Prof. Dr.-Ing. habil
Ruhr Uni Bochum, LAT
Sergii Nizhankovskyi, Dr.
Pavlo Konevskyi, Dr.
Igor Pritula, Prof. Dr. Sci.
Institute for Single Crystals,
Kharkov, NASU
The above results were achieved with the support of Central Innovation Programme for small and medium-sized enterprises. Funding Nr. EP201456
Alexey Kuzmichev, Dipl.-Chem.
Alexander Weber, Dipl.-Phys.
Helene Dyck, Dr.
Impex HighTech GmbH
Thank you for attention!

## Slide 7
Silicon Welding:
Specific material properties
Yasumasa Okada Y.,Tokumaru Y.
J. Appl. Phys. 56, 314–320 (1984)
Thermal Expansion Coefficient Of Silicon:
Strong non-linearities in the welding operating range leading to thermal and mechanical instabilities:
Thermal shocks
Crack propagation
Possible explanation of the material failure in the welding trials?

## Slide 8
Sapphire-to-Sapphire Ultrashort
Pulsed Laser Bonding: Optimization, Characterization
Pressure mount
Optimization of Laser Parameters (Power, Pulse Duration)
Optical welding verification
SEM-image of the weld seam