## Slide 1: DESIGN AND ANALYSIS OF A CRYSTALLINE SILICON TRIANGULAR VERTICAL SPRING BLADES
ESRA ZERINA APPAVURAVTHER
GEO 600-MAX PLANCK INSITUTE FOR GRAVITATIONAL WAVE PHYSICS (AEI)- POST-DOC

## Slide 2: Motivation
For the ET-LF (low frequency) cryogenics suspension, achieving sensitivity at 10K requires crystalline materials. While both sapphire and silicon are candidate materials, we aim to work with crystalline silicon, using a new manufacturing method (WEDM-Wire Electrical Discharge Machining) to enhance surface stress and lower the resonance frequency (10 Hz) of the vertical spring blades, meeting the required sensitivity.
Artist's impression of the underground Einstein Telescope, a planned third-generation gravitational-wave detector.
© NIKHEF

## Slide 3: Why Crystalline Silicon for ET?
ET requires cryogenic components to reduce thermal noise in the interferometer.
Silicon stands out for its:
High thermal conductivity (esp. at 10–20 K).
High mechanical (breaking) strength (suitable for suspensions).
Low thermal noise.
Low optical absorption (suitable for substrate applications).

## Slide 4: SINGLE CRYSTAL Silicon database:
Website: https://wiki.et- gw.eu/ISB/MaterialsDatabase/DatabaseSuspensions

## Slide 5: Why are crystalline vertical blades needed ?
Our concept of the ET-LF test masses involves employing a cryogenics suspension system that utilizes flexural joints combined with rectangular cross section rods.
The silicon blades lower resonance frequency and provide compliance for load distribution compensate for beam length tolerances.
My initial goal is to optimize the blade geometry in ANSYS to reduce mechanical stress and enhance natural frequencies, incorporating a new manufacturing method to further improve surface stress on the blade (Figure 1).
Figure 1. Isometric view with detail of test and intermediate mass (Scheme made by CSULA team of the suspension solution).

## Slide 6
We can solve all other “output” parameters, including:
As a starting point for blade design purposes, we choose the following fixed “input” parameters:
(1) Clamping angle (θ)
(2) Blade thickness (t)
(3) Natural frequency (f)
(4) Tip stiffness (k)
Mathematics of ideal triangular blade springs with small deformation

## Slide 7: Parameter optimization
Our initial investigation focuses on blade dimensions:
Length (150mm, 175mm, 200mm, 225mm),
Width (50mm, 75mm, 100mm),
Thickness (5mm-20mm).
Simulations involve loads:
100kg-1000N,
50kg-500N.
Figure 2. Von-Misses Stress Distribution (MPa) upper view of the intermediate mass crystalline silicon triangular blade spring.

## Slide 8: SILICON’s BREAKING STRENGTH
The blade's design aims to maintain stress well below the silicon's yield tensile stress.
The tensile stress causing silicon cantilever blade breakage was measured at approximately 270±75 MPa (Table 1).
To ensure safety, a maximum allowable tensile stress of 90 MPa is applied, considering a safety factor of 3.
Table 1. Results of breaking stress measurements on rectangular samples (10<L<20cm, thickness>2mm) done at Nikhef (2013).

## Slide 9
Surface stress
The tensile stress of 90 MPa is applied, considering a safety factor of 3.
Thicker blades show lower stress.
3x safety factor

## Slide 10
Natural frequency
Thicker blades have higher natural frequencies.
Design with less than 10Hz natural frequency.

## Slide 11: Experimental setup
The research aims to identify conditions that result in the maximum feasible stress for crystalline silicon flexures.

## Slide 13: How to calculate the bending stress of the flexures
An experimental setup has been prepared at Nikhef to measure stress (Figure 3).
This setup measures compression distance, compression force, height of the flexure, and the rotation angle at the end of the flexure, as shown in Figure 4.
Figure 4. Drawing of the experimental setup.
Figure 3. Photograph shows the height measurement process.

## Slide 14: WEDM cut strategy
Strategy:
Half of the samples will be cut along the <110> axis, with a breaking stress of 270 MPa (Table 1).
Due to the triangular design, cuts solely along <110> are impractical, so we will also test samples at a 13-degree angle to simulate tapering (Figure 5).
Wafers are 100 mm diameter, 300 µm thick, double-side polished, N-type (Sb) doped, with resistivity 0.008 to 0.02 ohm-cm, oriented <100>. Electrically conductive
WEDM: thin wire and electrical sparks to cut hard materials like metals or crystals without touching them (complex shapes with high accuracy).
Figure 5: Cutting Strategies: <110> and 13-Degree Inclined Sections
The electrical sparks between the wire and the material can only occur if the material allows current to flow.

## Slide 15: WEDM chemical etching
a-)
b-)
c-)
Figure 6: Optical microscope images of silicon samples:
a-) Sample with no chemical etching (non-crystalline surface),
b-) Chemically etched at 60°C for 20 minutes,
c-) Chemically etched at 60°C for 40 minutes.
45% weight potassium hydroxide (KOH) solution at 60°C is used for chemical etching, following the indications of Reynaerts et al.

## Slide 16: Results of the breaking strength measurements
Sample | Mean (MPa) | Standard Deviation (MPa)
SSP-90 (1.group) | 438.07 | 35.75
DSP-90 (2.group) | 348.76 | 49.38
DSP-13 (3.group) | 346.14 | 90.66
DSP-13 shows the lowest fracture strength and the widest spread in failure stress, indicating the least predictable mechanical performance.
DSP-90 has slightly higher strength and less scatter than DSP-13, but still underperforms compared to SSP-90 in both strength and consistency.
Fracture strength: the maximum stress a material can withstand before breaking.
Toughness: the ability to resist fracture by absorbing energy.

## Slide 17: Weibull Distribution Analysis of Silicon Samples Breaking Strength
Figure 3. The Weibull distribution parameters for the breaking strength (MPa) of crystalline silicon samples.
SSP-90 has the highest fracture strength (453.86 MPa) and most uniform mechanical behaviour (shape 16.71).
DSP-90 has moderate strength (351.30 MPa) and shows more scatter in strength values (shape 6.68).
DSP-13 has the lowest strength and the widest spread in failure stress (shape 5.57), making its performance less predictable.
(higher shape = less variability), and the scale parameter indicates the material's characteristic strength.

## Slide 18
Silicon blades capable of carrying 100-kg and 50-kg have been designed and optimized by FEA.
Designs with a natural frequency of less than 10 Hz and a peak stress of 90 MPa have been proven feasible.
The study is complemented with experimental tests on (smaller and thinner) WEDM samples measuring the breaking strength.
SSP-90 has the highest breaking strength, DSP-13 has the lowest breaking strength and highest variability, while DSP-90 is slightly stronger.
SUMMARY

## Slide 19: Backup slights

## Slide 20: Weibull distribution
The Weibull distribution models material failure and reliability using:
Shape parameter (β):
  β < 1 → early failures
  β = 1 → constant failure rate
  β > 1 → failure rate increases with time (e.g., wear-out)
Scale parameter (λ):
  Larger λ → higher strength or longer life
  Smaller λ → earlier failure or lower strength

## Slide 21: What we need for Design?
Size-Thickness
Aspect ratio (length/width)
Edge design (base of the blade)
Material properties (crystal orientation)
Support and fixturing
Load distribution (tip stiffness)
Environmental factors (cryogenics)
Testing and simulation

## Slide 22: But we need more for the design..
Material Selection
Crystal Orientation
Geometry
Blade Profile: blade's cross-section
Cryogenic Constraints
Stress Distribution
Natural Frequency
Thermal Analysis
Mounting and Attachment (assembling)
Material Properties
Load Conditions
Analysis Methods: FEA
Safety and Reliability
Manufacturability
Cost Constraints

## Slide 23: New blade design- Calstate senior design team

## Slide 24
Vertical directional deformation
Thicker blades has lower displacement under applied loads.

## Slide 25: Clamping angle
A higher clamping angle and increased applied load generally enhance stability and improve stress distribution.

## Slide 26: Stiffness
Stiffness increases with thicker blades.
Stiffness is a measure of how much a material resists deformation when a force is applied (k = F/Δx).
In simple terms: High stiffness = bends or stretches very little under load Low stiffness = bends or stretches more easily

## Slide 27: Why Crystalline Silicon for Cryogenic Suspension?
Seismic & thermal noise → limit GW detector sensitivity (<10 Hz) (Seismic: ground vibrations | Thermal: atomic motion)
Cryogenic operation → reduces thermal noise (Cryogenic: low temperature ~10 K)
Silicon → high thermal conductivity (efficient heat removal), low thermal expansion (dimensional stability)
→ high Q-factor (low mechanical loss = less thermal noise) [Q-factor: energy storage efficiency]
→ suitable for vertical spring design for ET-LF (Einstein Telescope Low Frequency)

## Slide 28: What makes triangular blade geometry effective?
Triangular shape → distributes stress evenly (Stress: internal force per area)
→ high rigidity near clamp, flexible at tip (Rigidity: resistance to bending)
→ tunes vertical resonance frequency < 10 Hz (Resonance frequency: natural vibration point)
→ compatible with compression-mode design, reduces stress peaks (Compression: force inward)

## Slide 29: How do mechanical losses affect thermal noise?
Thermal noise ∝ Temperature × Loss Angle / Frequency (Loss Angle φ: internal friction)
High mechanical loss → higher thermal noise → less sensitivity
Silicon at 10 K → very low φ → less thermal vibration (10^8 Q-factor)
Fluctuation-Dissipation Theorem → connects φ to thermal noise (FDT: noise-loss relationship)

## Slide 30: What challenges arise in fabricating silicon blades?
Silicon = brittle → machining introduces cracks (Brittle: breaks without bending)
WEDM (Wire Electrical Discharge Machining) → enables precision cutting
→ but causes micro-cracks → solved with chemical etching (Etching: removes damaged layer)
Surface quality critical → influences fracture strength and Weibull distribution (Weibull: failure probability model)

## Slide 31: How does anisotropy affect blade behavior?
Silicon = anisotropic → properties vary with orientation (Anisotropic: direction-dependent)
Crack propagation and toughness vary by crystal plane (e.g., <100>, <110>)
<100> chosen → higher toughness, balanced stiffness (Toughness: resistance to crack growth)
Orientation affects stress concentration and failure risk
Different crystal orientations (like <100> and <110>), have different resistance to crack growth (called fracture toughness).
Cracks may propagate more easily along one direction than another because of how atoms are arranged in the crystal, so the toughness isn't the same in all directions.
In short: Fracture toughness depends on crystal orientation. Some directions resist cracking better than others.

## Slide 32: How do your simulations and experiments match?
FEA (ANSYS) → simulates stress, deformation, resonance (FEA: Finite Element Analysis)
Boundary conditions = fixed clamp + tip load (Load: applied force)
Validated with bending tests → 3-point method, optical crack inspection
Surface stress < Breaking strength → confirms design feasibility

## Slide 33: What’s the broader impact on gravitational-wave detection?
Improved vertical isolation → better sensitivity below 10 Hz
Reduced thermal noise → clearer mid-frequency signals (10–100 Hz)
Supports ET’s goal → observe earlier-universe events & low-mass binaries
Silicon blade system = scalable, cryogenically optimized, experimentally validated

## Slide 34: Why are silicon's thermal properties important for cryogenics?
High thermal conductivity → essential for extracting heat from the payload (conductivity: heat flow ability)
Low thermal expansion → maintains dimensional stability when cooling (expansion: size change with temperature)
Zero-crossing near 18K and 123K → minimizes stress buildup during cool-down
→ Enables safe integration with other components at cryogenic temperatures

## Slide 35: How do you ensure blades don't fracture in real operation?
Weibull distribution → models statistical fracture probability (Weibull: failure likelihood)
Design ensures surface stress << breaking strength (Safety margin: stress limit buffer)
Fracture toughness orientation-dependent → <100> chosen for better resistance
Post-processing (etching) reduces surface flaws → enhances mechanical integrity

## Slide 36: What affects crack growth in single crystal silicon?
Crack follows cleavage planes → different for each orientation (Cleavage: natural break path)
Silicon is brittle → no plastic deformation → cracks propagate easily under tension
<111> prone to cleavage → <100> preferred for better toughness
Crack initiation sites often caused by machining defects → removed by etching

## Slide 37: How reliable are your FEA results in predicting real behavior?
Used nonlinear static + modal analysis in ANSYS (FEA: simulation method)
Input cryogenic material properties manually (e.g., Young's modulus at 10K)
Validated with experiments: bending tests, crack inspection, displacement tracking
Convergence study → ensured mesh independence of results

## Slide 38: What are the challenges in scaling your design for ET?
Larger mass → higher blade load → higher stress (Scaling: design adaptation)
Thermal contraction mismatch with other materials → needs compliant joints
Suspension dynamics more complex → needs active damping or feedback loops
Full system tests needed (ET-Pathfinder) → verify integration and performance