## Slide 1: III Workshop on ET-LF TM Tower Integration LNF Activities
Elba
September 29th -30th, 2025
L. Spallino, M. Angelucci and R. Cimino
LNF-INFN

## Slide 2
GW detector Upgrade for High Sensitivity
Frost mitigation on Cryogenic Mirrors
Electrostatic charges mitigation
Characterization of
materials vacuum properties
(Outgassing)
WP2
A. Liedl (Vacuum Group – Latino @ LNF
& MaSSLab & EGO/Virgo)
Identification and Control
of charge sources
(Electrostatic screen)
WP3
M. Angelucci (MaSSLab & Vacuum Group @ LNF
& EGO/Virgo & IFAE)
Frost Removal
(Electron desorption)
Charge mitigation
(Electron irradiation)
WP1
M. Angelucci (MaSSLab)
Cryogenic Environment
Passive
Active
Passive
Active
ET Activities @ LNF-INFN

## Slide 3
WP1: Frost mitigation and Electrostatic Charging (MaSSLab)
WP3: Passive mitigation method for electrostatic charging
(MaSSLab in collaboration with the Vacuum Group @ LNF, EGO/Virgo)
WP2: Material Properties (Vacuum Group @LNF in collaboration with MaSSLab and EGO/Virgo)
The aim of this WP is the characterization of the materials involved in the tower vacuum system containing the mirrors. The investigation of the outgassing properties will define the level and quality of vacuum surrounding the mirror surfaces.
The final goal of this WP is to validate the use of low energy electrons as a mitigation method for frost formation and as a neutralization method for mirrors’ electrostatic charging.
The aim of this WP is to carry out a R&D activity to develop a passive mitigation strategy for the electrostatic charging generated by low energy electrons coming from ion pumps, propagating along the beampipes and finally impinging on the test masses.
ET Activities @ LNF-INFN

## Slide 4
GW detector Upgrade for High Sensitivity
Frost mitigation on Cryogenic Mirrors
Electrostatic charges mitigation
Characterization of
materials vacuum properties
(Outgassing)
WP2
A. Liedl (Vacuum Group – Latino @ LNF
& MaSSLab & EGO/Virgo)
Identification and Control
of charge sources
(Electrostatic screen)
WP3
M. Angelucci (MaSSLab & Vacuum Group @ LNF
& EGO/Virgo & IFAE)
Frost Removal
(Electron desorption)
Charge mitigation
(Electron irradiation)
WP1
M. Angelucci (MaSSLab)
Cryogenic Environment
Passive
Active
Passive
Active
ET Activities @ LNF-INFN

## Slide 5: Activity at LNF-INFN

## Slide 6: Cryogenic Vacuum Issues on GWD optics
Water Layer Thickness [m]
From KAGRA experience, simulations indicate:
reflectivity gets affected, already after 100 nm of H2O ice
ET maximum thermal budget (~100 mW/ 1 W) is expected to be exceeded already after ~1-10 nm of H2O ice!!!
   Can we cure it?

## Slide 7: Residual gas adsorption on cold surfaces
Saturated vapour pressure from Honig and Hook (1960)
Cryosorption depends on:
surface temperature
pressure
gas partial pressures
They have to be correctly evaluated, considering:
PRT≠PLT (thermal transpiration correction)
vacuum history
For T~10 K and p<10-10 mbar, the most common residual gas species in a UHV chamber (except H2 and He) will be adsorbed, forming a molecular ice (“frost”) on the surface

## Slide 8: Residual gas adsorption on cold surfaces
The right evaluation of gas pressure allows to give reliable estimates of ice thickness forming on the cold surface.
Langmuir (L) unit:
1 L = 1x 10-6 mbar x 1s
gas exposure of a surface (or dosage)
For sticking coefficient Sc= 1:
1 L ~ 1 Monolayer (ML) cryosorbed
for H2O, 1 ML ~ 0.3 nm
 In 1x 10-12 mbar, it takes 1.000.000 s (~300 h / ~13 days) to build up a ML.

## Slide 9
R. Dupuy et al. J. Appl. Phys. 128, 175304 (2020)
L. Spallino et al., Phys. Rev. D, 062001, 104 (2021)
Electrons efficiently induce molecular ice nonthermal desorption!
Mirror
Low energy electrons irradiation
Possible if a charging mitigation method compliant with cryogenics is proved!

## Slide 10: Electrostatic charging on test masses of GW detector
Unclear in origin, quantity and even sign
Effects of charging:
Interferers with optical position control
Accumulation and motion of charges can generate fluctuating electric fields that could move the test mass at frequencies in the interferometer's sensitive band
Attracts dust, reducing reflectance, increasing scattering and absorption
Potentially limiting noise source
Electric field noise coupling to test mass motion

## Slide 11
Status of Activities:
Frost mitigation and Electrostatic Charging
Electrostatic charging neutralization by low energy electron irradiation:
Proof of concept (Spallino et al., PRD 2021; Spallino et al., PRD 2022).
Experimental validation at RT and LT (T~10 K) by developing a capacitive method for small prototypical samples (10 x 10 mm2) of metals, semiconductors and thin insulator layers (~20 nm) (Spallino et al., Vacuum 2025).
Frost mitigation by Electron Stimulated Desorption (ESD):
Efficient process already known in literature (Spallino et al., PRD 2021).
Capacitive setup developed for experimental validation
Electrons can neutralize both positive and negative charges by properly tuning their energy  ESD feasible in principle.
There is a strict correlation between neutralization parameters and SEY: by studying SEY features of any coating, it is possible to extract operational parameters to discharge it.
It is possible to induce a stable and homogeneous surface potential.

## Slide 12
Status of Activities:
Frost mitigation and Electrostatic Charging
Electrostatic charging neutralization by low energy electron irradiation:
Experimental validation at RT and LT (T~10 K) on more realistic small samples by capacitive method ( waiting for materials coming from collaboration)
Experimental studies on charge distribution and neutralization for big realistic samples (1-inch, thick insulators)  implementation of a dedicated setup equipped with a Kelvin probe (system currently under test).
Frost mitigation by Electron Stimulated Desorption (ESD):
First tests on H2O/Si and Cu to combine ESD and neutralization
Kelvin probe scheme under test for charging neutralization
Chamber inner view
e- gun
Sample holder
Kelvin probe
Setup overview

## Slide 13
Mid-term Perspective:
Frost mitigation and Electrostatic Charging
Preliminary XPS and Raman investigations carried out in our lab on prototypical small have shown that, within the detectability limit of these experimental techniques, electron irradiation below few hundreds’ eV does not induce observable structural defects on the substrate.
More investigation are needed, especially on realistic and specific materials.
 WHAT is the effects induced by electron irradiation on optics?
 WHAT is the best way to monitor the effects (studies on optical properties and/or noise induced effects: crystallization status, optical defects, scattering centers, scattering losses, mechanical losses,...)?
Work in progress within the ET-Italia collaboration (Core Optics and Coating group) but we are opened to inputs and suggestions!
Laboratory based experiments

## Slide 14
 At the present stage, can the method be integrated in design of the overall system? and HOW?
 WHAT is the impact at cryogenic conditions?
Frost mitigation and Electrostatic Charging
Final goal  Integration
Is there an available mock-up system where to plan test on:
frost/neutralization mitigation methods by using electrons;
effects on optics under realistic conditions;
If it is not, a mock-up system should be designed/realized.
Mandatory R&D plan
cold electron gun
a charging monitoring system
In principle, electron irradiation to mitigate charging is compatible with cryogenics and will work at RT as well.

## Slide 15
GW detector Upgrade for High Sensitivity
Frost mitigation on Cryogenic Mirrors
Electrostatic charges mitigation
Characterization of
materials vacuum properties
(Outgassing)
WP2
A. Liedl (Vacuum Group – Latino @ LNF
& MaSSLab & EGO/Virgo)
Identification and Control
of charge sources
(Electrostatic screen)
WP3
M. Angelucci (MaSSLab & Vacuum Group @ LNF
& EGO/Virgo & IFAE)
Frost Removal
(Electron desorption)
Charge mitigation
(Electron irradiation)
WP1
M. Angelucci (MaSSLab)
Cryogenic Environment
Passive
Active
Passive
Active
WP5 (2026)
M. Angelucci (MaSSLab)
Development of a
“Cold” electron gun
ET Activities @ LNF-INFN

## Slide 16
GW detector Upgrade for High Sensitivity
Frost mitigation on Cryogenic Mirrors
Electrostatic charges mitigation
Characterization of
materials vacuum properties
(Outgassing)
WP2
A. Liedl (Vacuum Group – Latino @ LNF
& MaSSLab & EGO/Virgo)
Identification and Control
of charge sources
(Electrostatic screen)
WP3
M. Angelucci (MaSSLab & Vacuum Group @ LNF
& EGO/Virgo & IFAE)
Frost Removal
(Electron desorption)
Charge mitigation
(Electron irradiation)
WP1
M. Angelucci (MaSSLab)
Cryogenic Environment
Passive
Active
Passive
Active
WP5 (2026)
M. Angelucci (MaSSLab)
Development of a
“Cold” electron gun
ET Activities @ LNF-INFN

## Slide 17
WP2: Material Properties
(Vacuum Group – Latino @ LNF in collaboration with MaSSLab & EGO/Virgo)
RGA
H2O
CO/N2
CO2
Outgassing and RGA data for a commercial Kapton insulated coaxial cable, suitable for cryogenic applications. (data to be published)

## Slide 18
Status of Activities:
Materials properties
The aim of this WP is the characterization of the materials involved in the tower vacuum system containing the mirrors. The investigation of the outgassing properties will define the level and quality of vacuum surrounding the mirror surfaces.
Two Chamber for samples (f 200 x 260mm and f 250 x 450mm)
Background ≈10-13 mbar/l s cm2; two RGA analyzer
LNF «LATINO» - Outgassing Facility - fully operating.
LNF-Virgo/EGO networking for materials’ characterization.
First tests on samples provided by Virgo/EGO to be in line with measurement methods and procedures
Coil
Baffle
We are ready to carry out measurements’ campaigns.
Material/devices proposed to be used in the tower vacuum system?
Networking with other outgassing facilities for database?

## Slide 19
GW detector Upgrade for High Sensitivity
Frost mitigation on Cryogenic Mirrors
Electrostatic charges mitigation
Characterization of
materials vacuum properties
(Outgassing)
WP2
A. Liedl (Vacuum Group – Latino @ LNF
& MaSSLab & EGO/Virgo)
Identification and Control
of charge sources
(Electrostatic screen)
WP3
M. Angelucci (MaSSLab & Vacuum Group @ LNF
& EGO/Virgo & IFAE)
Frost Removal
(Electron desorption)
Charge mitigation
(Electron irradiation)
WP1
M. Angelucci (MaSSLab)
Cryogenic Environment
Passive
Active
Passive
Active
WP5 (2026)
M. Angelucci (MaSSLab)
Development of a
“Cold” electron gun
ET Activities @ LNF-INFN

## Slide 20
Status of Activities:
Passive mitigation method for electrostatic charging
Limit free electron imping on optics
From the Virgo experience: Electrons coming from Ion pumps
Studies on the emitted electrons from ion pumps
Mes. Of Number of emitted electrons
Emission configuration
…
Studies on the electron’s propagation along the beampipe
Numerical simulation of propagation
Mes. of Number of propagated electrons
SEY of beampipes material

## Slide 21
Currents vs Ion pump voltage
Ion pump
K1
K2
Studies on the emitted electrons from ion pumps
(Applied
Voltage)
(Collector)
Electrostatic screens
Specific configuration for installation
 Mock-up system under construction

## Slide 22
 At the present stage, can the method be integrated in design of the overall system? and HOW?
Studies on the emitted electrons from ion pumps
Final goal  Integration
R&D activity LNF-EGO/Virgo to test the possibility of integrating an electrostatic ring on selected baffles to mitigate the charges’ flow.
R&D activity on final design of electrostatic screen considering pumping variation...

## Slide 23: Summary
We are at a critical point for activities related to frost and charging mitigation by electrons
 we believe it could be the right time to move towards an advanced phase requiring a well-defined R&D program involving the GWD community.
Even if we are ready, characterizations on outgassing properties of specific materials of interest are in stand-by
 a collective enterprise could be beneficial to push this activity in different laboratories (EU call?).
The work on passive strategy to mitigate electrostatic charging is promising and in line with time
 Interaction for integration/R&D
We are going on with our work program
Final goal  Integration
Mandatory R&D plan
Strong interaction with the community is needed

## Slide 25
Proof of concept
Electrons of variable but low energy (below few hundreds eV) can compensate charges of both polarity
Secondary Electron Yield
(SEY or d)
SEY=Iout/IIn
L. Spallino, IL NUOVO CIMENTO C (2022)
L. Spallino et al., Phys. Rev. D. (2022)
Charging mitigation by low energy electrons

## Slide 26
Incident electrons current (Ip)
Emitted electrons current (Iout)
Faraday cup
Sample
MaSSLab
Material Surface Science Laboratory @ LNF-INFN
UHV systems for multi-technique surface studies
main chamber
preparation
chamber
fast-entry lock
Electrostatic measurements
Capacitive setup developed for experimental validation

## Slide 27
Electrons can neutralize both positive and negative charges by properly tuning their energy.
There is a strict correlation between neutralization parameters and SEY: by studying SEY features of any coating, it is possible to extract operational parameters to discharge it
From a proof of concept to the experimental validation
L. Spallino et al., Vacuum (2025)
Ongoing electrostatic measurements
L. Spallino et al., To be published

## Slide 28
S. Tanioka et al., Phys Rev. D (2020)
Cryosorption on cold optics (frost)
S. Tanioka and Y. Aso, Optic Express (2021)
From KAGRA experience, simulations on ET indicate:
reflectivity gets affected, already after ~100 nm of H2O ice
Dramatic effects on optical properties
Water Layer Thickness [m]
K. Hasegawa et al., Phys Rev. D (2019)

## Slide 29
R. Dupuy et al. J. Appl. Phys. 128, 175304 (2020)
L. Spallino et al., Phys. Rev. D, 062001, 104 (2021)
Electrons efficiently induce molecular ice nonthermal desorption!
Mirror
Low energy electrons irradiation

## Slide 30: Low energy electrons irradiation
Mirror
If Peff ~ 1x10-10 (H2O,CO,CO2, etc) mbar; sticking coefficient = 1
1 monolayer (~ 1015 mol/cm2 ~ 0.3 nm) will be cryosorbed in 10.000 s.
(~ 2.5nm/day ~ 10 times less than in KAGRA)
If we assume a mean ESD h= 0.1 mol./electron (as for H2O) @ 100eV.
(R. Dupuy et al. J. Appl. Phys. 128, 175304, 2020)
To remove 1 ML we need an el. current of: ~ 1 mAmps/cm2 in one second
… depositing less than 100 mW/ML/cm2 (not all el. energy goes in thermal heat!)
All in UHV, with marginal heating up of the mirrors and (possibly) reduced downtime.
Deserves further investigation!

## Slide 31
WP2: Material Properties
(Vacuum Group – Latino @ LNF in collaboration with MaSSLab & EGO/Virgo)
Saturated vapour pressure from Honig and Hook (1960)
The main factor determining the vacuum level within the towers is the amount of gas released from the components installed inside the tower's chambers.
 The choice of materials is critical to limit the traces of low-volatile organics, potentially cryosrobing onto optical surfaces and directly degrading ET performances.
Test on materials and assemblies to assess their compatibility to the vacuum
Outgassing Measurements
Vacuum compatible Materials List (EGO-INFN-KIT MoA)

## Slide 32
Studies on the emitted electrons from ion pumps
Ion Pump
Collector 1
Collector 2
UHVacuum Chamber
Collector
Emitted
electrons