## Slide 1: Status of crystalline monolithic suspension for ET-LF
Michele Arcangelo Dicorato, Nicolo’ Baldicchi, Flavio Travasso – University of Camerino, University of Perugia
Ardiana Nela (IGR) – University of Glasgow
Iryna Buchovska, Robert Menzel – Institut für Kristallzüchtung, Berlin
Gravitational Waves and Detection Technologies - PAS Rome meeting 2026

## Slide 2: Outline
Why crystalline test-mass suspension
Production
Fibers characterization
Blade simulations
  Michele Arcangelo Dicorato and Nicolò Baldicchi, PAS Rome meeting 2026

## Slide 3
Monocrystalline silicon is one of the most promising candidate materials.
This is due to its thermoelastic nulling regions (zero crossing of the thermal expansion coefficient at 18K and 123K) and low mechanical loss at cryogenic temperatures.
Blade
Ear
Substrate
Marionette
Fiber
Anchor
Heat load
Mirror mass 211 kg
SUSPENSION REQUIREMENTS:
High thermal conductivity
High breaking strength
Low mechanical loss (loss angle )
Low resonant frequency (< 2 Hz)
220 MPa with a safety factor of 3
Low thermal noise
Cryogenic temperature (10 K -20 K )
Excellent surface quality
  Michele Arcangelo Dicorato and Nicolò Baldicchi, PAS Rome meeting 2026
Towards the development of a silicon cryogenic suspension

## Slide 4
LEIBNIZ - INSTITUT FÜR KRISTALLZÜCHTUNG
Crystal
HF
Inductor
Feed
Melt
Pulling
Pulling
Pedestal growth
Float zone growth
Float-zone technique produces high purity, contaminant free, single crystal uniform silicon fibers with exceptionally good surface quality.
A silicon feed rod is melted at the bottom using an inductive coil
The molten zone contacts a monocrystalline seed
The seed is moved downwards, and crystallization begins
Molten silicon solidifies into a large single crystal silicon fiber without direct contact with seed rod, minimizing impurities
  Michele Arcangelo Dicorato and Nicolò Baldicchi, PAS Rome meeting 2026
Fiber production
Notes: Si-fiber diameter: 3 mm
Diameter variation: +/- 0.1 mm
Length: up to 1.5 m
Reproducible process with low fiber-to-fiber variation

## Slide 5
Long fibers with grown thicker ends
Welding of 3 mm rods
Welding of 8 mm rods
  Michele Arcangelo Dicorato and Nicolò Baldicchi, PAS Rome meeting 2026
Fiber production

## Slide 6
Mechanical loss measurements
Mechanical loss measurements at the University of Camerino to accurately measure the loss of fibers with the ring-down method
Clamp material (rigidity, density)
Clamp dimensions
Fastening strength
If the fiber has an excellent surface quality and a good crystallinity, the limiting factor for this measurement at cryogenic temperature is the clamp loss
[Douglas M. Photiadis and John A. Judge Attachment losses of high Q oscillators]
  Michele Arcangelo Dicorato and Nicolò Baldicchi, PAS Rome meeting 2026
Fiber characterization

## Slide 7
Tensile stress measurements
Vertical Alignment with micrometric controls and laser level
Fiber with seed
(Perugia method)
Fiber without seed
(Glasgow method)
Work done with Ardiana Nela and Dr Flavio Travasso at the University of Perugia
  Michele Arcangelo Dicorato and Nicolò Baldicchi, PAS Rome meeting 2026
Fiber characterization

## Slide 8
Bending system designed and optimized for cylindrical rods 3 mm thick and 5 cm long, according to the standard ASTM C1684-18 2023
[Quinn et al., Journal of Testing and Evaluation, 2009]
2a
4-point bending method
Work done with Ardiana Nela and Dr Flavio Travasso at the University of Perugia
Why bending test?
To determine the assembly precision (some misalignment in the assembly can cause the fiber to bend)
To determine the dynamic displacement range during the setup of the active controls
Maximum tensile stress
  Michele Arcangelo Dicorato and Nicolò Baldicchi, PAS Rome meeting 2026
Fiber characterization
Bending stress measurements

## Slide 9
Data dispersion on tensile tests is most likely due to imperfection on the fibers (microcracks) caused by a not optimal shipping and handling technique
The good news is that fibers don’t break at the welding point
  Michele Arcangelo Dicorato and Nicolò Baldicchi, PAS Rome meeting 2026
Tensile tests

## Slide 10
Lower dispersion but still some outliers
From the high speed camera we can see that the break is due to a microcrack on the surface of the fiber
  Michele Arcangelo Dicorato and Nicolò Baldicchi, PAS Rome meeting 2026
Bending tests

## Slide 11
GOOD SAMPLE
OUTLIER
  Michele Arcangelo Dicorato and Nicolò Baldicchi, PAS Rome meeting 2026
Bending tests

## Slide 12
Tensile data
Same production process but different handling and shipping:
red data = old, blue data = new
  Michele Arcangelo Dicorato and Nicolò Baldicchi, PAS Rome meeting 2026
Handling comparison

## Slide 13
Why? Attenuation of noises that causes the vertical displacement of the test mass
How? Magnetic anti spring (MAS) or geometric anti spring (GAS)
[Mathieu Blom PhD Thesis]
[Extending the VIRGO gravitational wave detection band
down to a few Hz: metal blade springs and magnetic antisprings, M. Beccaria et al. ]
  Michele Arcangelo Dicorato and Nicolò Baldicchi, PAS Rome meeting 2026
Blades
Future? Monolithic geometric anti spring

## Slide 14
Finite Linear Element Connected in Series (FLECS): a simulation tool for geometric anti-springs
(with P.Chessa)
x
θ_i
θ_f
Divide the blade in N finite elements and set the geometric constraints
Compute potential and kinetic energy and find static equilibrium minimizing
Build Hessians and solve the generalized eigenvalue problem
  Michele Arcangelo Dicorato and Nicolò Baldicchi, PAS Rome meeting 2026
Blades
Output:
Blade profile at equilibrium
Maximum stress in each element
Modal frequencies
Eigenmodes

## Slide 15
This allows to do parametric scans for blade prototyping
  Michele Arcangelo Dicorato and Nicolò Baldicchi, PAS Rome meeting 2026
Blades

## Slide 16
  Michele Arcangelo Dicorato and Nicolò Baldicchi, PAS Rome meeting 2026
Conclusions
A big international effort is being put into research and development of suspension components for ET-LF
The float zone has been proven to be a very reliable production technique for silicon fibers
Breaking tests have improved but samples handling and shipping methods need to be improved
The collaboration is starting to work also on research and development of spring blades
The nexts step will be to experimentally characterize alternative spring blades arrangements in geometric anti spring configurations

## Slide 17
  Michele Arcangelo Dicorato and Nicolò Baldicchi, PAS Rome meeting 2026
Thank you for your attention!

## Slide 18: Supplementary slides

## Slide 19: Losses in a pendulum
The energy stored in gravity is lossless and dominates in heavily loaded suspension fibers. This implies that the pendulum loss is lower than that of the material used for the suspension fiber: the only mechanical loss in each cycle is of the total energy stored in the oscillating rod.
n: number of wires
E: Young’s modulus
T: tension of the wire
In the high frequency limit
Pendulum thermal noise goes like
A similar analysis shows that goes also like
Why large and heavy mirrors?
To keep the radiation pressure effect low
To allow large-sized beam spots on the mirror surfaces for lowering thermal noise
Dilution factor

## Slide 20: Suspension thermal noise
Bulk loss-angle at 10 K:
Silicon <100>
4 wires
Length: 1,2 m
Diameter: 3 mm
Mirror mass: 211 kg
Average temperature: 15 K
Pendulum mode
First violin mode
Notes: These are the current baseline parameters, with which the suspension thermal noise is actually below the required sensitivity curve of ET.

## Slide 21: Sensitivity of ET
ET-LF sensitivity curve
ET sensitivity curve
Notes: On the left is shown the expected sensitivity curve of ET, as the sum of the curves of the two interferometers. On the right is shown the ET-LF sensitivity curve as a dark line, which is the sum of all the noise contributions that are marked in color.
Thanks to the multistage pendulum suspensions the influence of seismic noise can be limited to the frequency range below 2 Hz.
The operation at cryogenic temperatures reduces the influence of suspension thermal noise in the frequency range above 7 Hz to below the quantum noise
Below 7 Hz the sensitivity is limited by quantum noise, newtonian noise, and suspension thermal noise.

## Slide 22: Rod sizing
Mirror temperature as a function of marionette temperature for some rod diameters, considering 4 silicon rods of length 1,2 m and a heat load of 0,5 W
CURRENT DIAMETER BASELINE CHOICE: d = 3 mm
Notes: Increasing suspension diameters results in better heat extraction and a lower mechanical stress, despite a higher suspension thermal noise. The current choice for the rods is a diameter of 3 mm.
Considering a heat load of 0,5 W, to keep the mirror within a temperature range between 15 K and 20 K, the marionette must be within a temperature range between 7.5 K and 15.5 K.

## Slide 23: Rod sizing
4 wires of 3 mm diameter
211 kg mirror
Stress on each wire = 73 MPa
Safety factor of 6
439 MPa tensile strength
High variability in the breaking strength measurements
Improvement of production process and breaking strength measurements to reduce the safety factor.
BREAKING STRENGTH
LENGTH
A decreasing length yields a reduction of temperature of the mirror, but also shift all the modes to higher frequencies.
Constraint imposed by the tower dimensions and cryostat dimensions
CURRENT REFERENCE LENGTH: 1,2 m
Notes: With 4 wires of 3 mm diameter supporting a 211 kg mirror, the stress on each wire is 73 MPa. Since there is still high variability in the measurements of breaking strength, in order to consider strength uncertainties, we apply a safety factor of 6. In this case we must have a tensile strength of at least 439 MPa. Improving the production process and the breaking strength measurements the reliability of the fibers would increase and the safety factor could be reduced.

## Slide 24: Profiler