## Slide 1: Laser Technologies
Marco Galimberti
European Gravitational Observatory

## Slide 2: Summary
Main Laser
Light Amplification and Laser Amplifier
Laser Oscillator
Amplification, Beam Cleaning & VIRGO Main Laser
Non Linear Optics
Second Harmonic Generation
Pockels Cell
Faraday Isolator
Sound and Light
Acousto-Optic modulator
Brillouin Instability
Laser Safety
Be Careful

## Slide 3: Main Laser

## Slide 4: Two Level System
With a two level system, an e- at ground state can absorbe some light resonant with the transition and go to the excited state
0
E1
0
E1
From the excited state it can emit some light at the transition frequency by spontaneous emission (QED)
0
E1
0
E1
From the excited state, if there is some light resontant with the transition it can emit the same light, with stimulated emission
0
E1
0
E1

## Slide 5: Light Amplification
If there are more e- on the upper state compared to the ground state, there is inversion of population and there is light amplification
If we pump a two level system with light, it is impossible to have population inversion
With optical pumping, at least 3 level are needed, 4 are better
Pumping with other method, like current on semiconductor junction (laser diode)
Photon
e-
E0
E3
E1
E2
Photon
Photon
Photon
e-
E0
E3
E1
E2
Photon
Photon

## Slide 6: Small Signal Gain and Saturated Gain
The lifetime of excited state is called fluorescence time
The small signal gain of an amplifier is , where is the store fluence in the amplifier, is the saturation fluence and is the transition cross section
If the intensity of the incoming light is not small, the gain is reduced by
If the input intensity is comparable or higher then , the amplifier will be depleted
where
Homogeneous Line

## Slide 7: Amplification Bandwidth
Each absorbtion or emission line has a bandwidth
The laser line bandwidth is important for the type of the laser we want
Two different type of line:
Homogeneous
Inhomogeneous
The bandwidth is defined by the transition
All the excited atoms will resonate at the same light frequency
The overall bandwidth is defined by the material
There are different population of atoms, with the transition line shifted (by Stark Effect, Doppler, etc)
Different atoms will resonate at different light frequency

## Slide 8: Laser Materials
Nd:YAG at 1% of doping
Inhomogenous Line
Er:Yb Glass
Inhomogenous Line

## Slide 9: Nd:YAG
Absorption and emission spectra for Nd:YAG took online
Not all the emission lines are laser lines!
946 nm
1064 nm
1123 nm
1319 nm
1338 nm
1415 nm
1444 nm
Laser Lines

## Slide 10: Nd:YLF
Absorption and emission spectra for Nd:YLF took online
Not all the emission lines are laser lines!
1047 nm
1053 nm
1313 nm
1324 nm
1370 nm
Laser Lines

## Slide 11: Laser Amplifier
Active Medium
Power
Power
Input beam
Output beam

## Slide 12: Optical Pump Scheme
Flash
Flash
Laser pump (diode or another laser)
High efficiency, optimal pumping wavelenght
Flash (or arc lamp)
No efficiency, high thermal load
Only good for high energy pulse laser
Diode
Diode
Diode
Diode
Side pumping
Diode
Head on pumping
fibre
Diode
Fibre Amplifier
There is gain only where the medium is pumped
The gain depend on the intensity of the pump

## Slide 13: MOPA Architecture
MOPA: Master Oscillator Power Amplifier
The Oscillator create the laser beam with the desired parameters at low power
The Amplifiers increase the power up to the desired level
Telescopes are required to increase the beam size to avoid damages
Back propagating light needs to be blocked to avoid damages and/or malfuctioning by using a Faraday isolator
FR
Oscillator
FR
Amplifier
Amplifier

## Slide 14: Laser Oscillator
A laser oscillator is a laser amplifier in a cavity
For a nice laser beam (single mode) the cavity needs to be stable
From the saturation intensity, it is almost impossible to have a laser oscillator with high power output (tens of W)

## Slide 15: Cavity and Modes
A stable cavity allows many modes to oscillate
where is the free spectral range, is the round trip optical pathlength and is the round trip Gouy phase
For a cavity , to be compared with the Nd:YAG bandwidth (about 500 modes)
Trasversal mode could also oscillate, unless they are suppressed by spatial filtering

## Slide 16: Homogenous Medium
At the start many mode can oscillate because the gain of the medium is high and the light intensity inside the cavity is small compared to the Isat
Increasing the intensity of the light, the gain is reduced by the saturation for all the mode
Only few modes (or one) could be mantained on the steady state

## Slide 17: Inhomogeneous Medium
At the start many mode can oscillate because the gain of the medium is high and the light intensity inside the cavity is small compared to the Isat
Increasing the intensity of the light, the gain is reduced by the saturation almost independently for each mode. Each atom population resonating with the mode frequencies will be depleted creating a hole in the gain spectrum
Many mode can oscillate

## Slide 18: Spatial Hole Burning
In a linear cavity, the field is a standing wave inside the laser medium
The laser medium will saturate where there is constructive interference
Gain remain high on the node, promoting other modes

## Slide 19: Single Longitudinal Mode Laser
International Journal of Optics, Volume: 2021, Issue: 1, First published: 28 July 2021, DOI: (10.1155/2021/6667015)
To avoid multiple longitudinal modes to oscillate it is necessary to:
reduce the number of mode inside the gain bandwidth by increasing the free spectral range, i.e. short cavity;
reduce the small signal gain;
suppress unwanted modes, i.e. adding an etalon in the cavity
avoid hole burning by using ring cavity

## Slide 20: And for the Transversal Modes?
Higher transversal mode can oscillate in a cavity
Depending of the Gouy phase, they can have different frequency so they can be suppressed as the other longitudinal mode
They are in general larger than the TEM00 mode
They can be suppressed by:
an aperture inside the cavity (hard spatial filtering);
pump the active medium only for the area used by the TEM00 (soft spatial filtering).
Holgado, Warein & Sola, I. & Jarque, Enrique & Jarabo, Sebastián & Roso, Luis. (2012). Q-switching in a neodymium laser. EUROPEAN JOURNAL OF PHYSICS. 33. 265-278. 10.1088/0143-0807/33/2/265.

## Slide 21: Nonplanar Ring Oscillator
Commercial Nd:YAG single mode oscillator uses ring cavity
Compact monolitic design ( and )
The laser can only oscillate on one direction by the 3D geometry and the reflections on 2, 3 and 4, at Brewster angle.
Pumped by a diode laser
Frequency is controlled by pressing the Nd:YAG on the side and/or changing the temperature
Output power

## Slide 22: Slave Laser
A free space amplifier can amplify a laser beam but it can not filter higher modes
An oscillator can provide a nice beam but it is limited by the power
A low power oscillator can be used to seed an high power slave oscillator
The mode in the slave is forced by the seed (on a small range spectral range)
The slave cavity provides good beam quality and power () while the seed provides spectral quality

## Slide 23: Beam Cleaning
The beam at the end of the laser system is not perfect
Power fluctuation: the power could be stabilized using a feedback loop
Spatial and spectral beam quality: a filter cavity can be use to filter only the TEM00 and the main spectral line
Beam position and pointing: automatic alignment of two mirrors
On other laser system, phase front quality could be improved by a deformable mirror

## Slide 24: VIRGO Main laser
Nd:YAG
NPRO Oscillator
Slave Oscillator
Amplifier
Pre Mode Cleaner

## Slide 25: VIRGO Main Laser

## Slide 26: VIRGO Main laser

## Slide 27: And for Higher Power?
The main problems are:
Provide pump power: for a 1kW laser you need to provide around 2kW of pump
Thermal managment: high power imply more thermal lenses, stronger cooling system is needed
Avoid damages: larger beams are needed, around 10mm (Thorlabs), more space, alignment more critical, etc
Beam quality: more optical components can degradate the beam quality
Reliability: complex system are more difficult to mantain

## Slide 28: Possible Technologies
Coherent beam recombination: add the power from many amplifiers
OSC
Preamp
Amp
Amp
φ
PMC
PID
Diode pumped rod amplifier
Thin disk laser amplifier
Large Area Fibre Amplifier: amplification in special fibre, photonic crystal
DC-200/40-PZ-Yb fiber
NKT Photonics

## Slide 29: Non Linear Optic

## Slide 30: Theoretical Framework
In general, the polarization is not necessary linear with respect the electrical field
Maxwell equations in a material are linear, most of the time
Any material has while only material without inversion symmetry has
Considering
is related to the refractive index;
If there is a term of oscillating at
If the refractive index is function of

## Slide 31: Second Harmonic Generation
+
With slow varing approximation and
NLO
z

## Slide 32: Second Harmonic Generation - 2
When , the conversion is quadratic with the length of the crystal

## Slide 33: Phase Matching
The have high SHG efficiency it is necessary to have , i. e.
This condition is called phase matching
Polarizations |  |  | Scheme
e | o | o | Type I
e | o | e | Type II (or IIA)
e | e | o | Type III (or IIB)
e | e | e | Type IV
o | o | o | Type V (or type 0,[21] or "zero")
o | o | e | Type VI (or IIB or IIIA)
o | e | o | Type VII (or IIA or IIIB)
o | e | e | Type VIII (or I)
Polarizations |  |  | Scheme
e | o | o | Type I
e | o | e | Type II (or IIA)
e | e | o | Type III (or IIB)
e | e | e | Type IV
o | o | o | Type V (or type 0,[21] or "zero")
o | o | e | Type VI (or IIB or IIIA)
o | e | o | Type VII (or IIA or IIIB)
o | e | e | Type VIII (or I)
Or…
All the SHG crystals are at least birefringent. By having the fundamental and the second harmonics with different polarization it is possible to tune one of the two refractive index by changing the angle of the crystal
For some crystals, the phase matching can be done by changing the temperature (non critical phase matching)
Efficiency also depend on , connected to the crystal and the polarization of the beams

## Slide 34: Quasi Phase Matching
Out of the phase matching, the conversion is periodic.
If after half of the oscillation we turn the crystal by 180°, the second harmonic is no going out of phase
Different crystals can be used, with less requirement on the phase matching and potentially higher non linearity
Tuning is done by changing the temperature
Those crystals are called Periodically Poled Crystals

## Slide 35: Crystals
Crystal | Phase‑matching type | deff (pm/V) | nω (1064 nm) | n2ω (532 nm) | PM angle (°)
KTP (KTiOPO₄) | Type II (most common) | ~3.4 | 1.8296 | 1.8873 | ~23° (θ, z‑type II)
LBO (LiB₃O₅) | Type I | ~0.8 | 1.606 | 1.622 | ~90° (xz‑plane)
BBO (β‑BaB₂O₄) | Type I | ~2.0 | 1.657 | 1.681 | ~22°
LiNbO₃ (LN) | Type I | ~4.5 | 2.223 | 2.286 | ~44°
KDP (KH₂PO₄) | Type II | ~0.4 | 1.505 | 1.520 | ~41°
CLBO (CsLiB₆O₁₀) | Type I | ~0.9 | 1.606 | 1.622 | ~75°
BIBO (BiB₃O₆) | Type I | ~3.2 | 1.79 | 1.83 | ~168°

## Slide 36: PP Crystals
Crystal | Poling Period Λ (µm) | deff (pm/V) | Damage Threshold | Temperature Range
PPKTP (Periodically Poled KTP) | ≈ 9.0 µm | ~9–10 (QPM‑enhanced) | Very high | Wide (room temp OK)
PPLN (Periodically Poled LiNbO₃) | ≈ 6.9 µm | ~15–17 (QPM‑enhanced) | Medium | Needs temp control (≈ 80–120 °C)
MgO:PPLN | ≈ 6.9 µm | ~14–16 | High | 50–150 °C
PPLT (Periodically Poled LiTaO₃) | ≈ 8.2 µm | ~10–12 | High | 30–200 °C
PPRbTiOPO₄ (PPRTP) | ≈ 8–9 µm | ~8–9 | Very high | Wide
PPMgSLT (Periodically Poled Mg‑stoichiometric LiTaO₃) | ≈ 8.0 µm | ~11–12 | Very high | 30–200 °C

## Slide 37: How to Improve the SHG Efficiency?
To increase the SHG, it is necessary to increase the pump intensity
The pump beam could be focused on the crystal, but the intesity is high only in the focal region
The SHG crystal could be placed inside a cavity with high Q for the pump
SHG
HR 1064nm
HR 532nm
HR 1064nm
AR 532nm

## Slide 38: Pockels Cell
Let consider again a non linear crystal with but with a static Electric field and a plane wave
+
The static electric field, if strong enough, can change the refractive index of the material for the plane wave
More important, it can change the refractive index for one polarization

## Slide 39: Pockels Cell - 2
If the polarization of the light is on the y axis, it can be used to change the phase of the beam
Let suppose that and
If the polarization of the light is at 45° with respect the y axis, it can be used change the polarization, up to turn it of 90°, and to modulate the amplitude
For
It requires 900V
LiNdO3
L
s
E
DKDP
E
L
For It requires 8kV

## Slide 40: Faraday Effect
Most of the optical devices are not able to stop back reflection
Back reflection can be dangerous for:
amplified laser system: back propagating beams can still be amplified;
oscillator and cavities: unwanted coupled cavities
Some material, with a strong magnetic field, turn the polarization of the light
The amount of rotation is proportional to the length of propagation and to the amplitude of the magnetic field

## Slide 41: Faraday Isolator
By turning the polarization by 45° and using two polarizers, back reflection can be blocked
The magnetic field is a Psedo-vector, a back propagating beam will have the polarization turned by the same amount

## Slide 42: Sound and Light

## Slide 43: Interaction Light – Sound
The density of a material with a sound wave of amplitude , pulsation and speed can be describe as
The refractive index is proportional to the density
A periodic variation of the refractive index act as a grating
Acustic wave
z
x
L

## Slide 44: Acousto Optic Modulator
Considering a plane wave of light into the sound wave
where
For small signal
We have 3 wave, the transmitted beam and 2 diffracted beams with different frequency
Acoustic wave
z
x
L

## Slide 45: Longitudinal Acoustic Waves
The acustic wave can also be collinear to the light propagation
In this case we have a volume Bragg grating
where
For small signal
If =2 the light is reflected back
Acoustic wave
z
x
L

## Slide 46: Brillouin Instability
With foward and backward light wave there is a standing wave, with periodic local intensity in z
If there is a gradient of the intensity there is a radiation pressure on the material
A periodic and oscillating force on the material can create or amplify a sound wave
The sound wave can reflect back the incoming light wave

## Slide 47: Phase Matching and Brillouin Shift
Considering: a sound wave of pulsation , wave vector q and phase velocity of ,
incoming light beam (Pump) of pulsation and wave vector ,
back reflected beam (Stokes) of pulsation and wave vector
If is small, then , and
and
The process is described by those equations, including absorption of the light and the sound wave

## Slide 48: Instability Threshold and Effects
Longer is the material, more is the gain; more is the Pump intensity, more is the gain
The instability is started by the noise. If the gain is enough, the process evolves to a steady state
Threshold formula
Some numbers for single mode Fused Silica fibre, core diameter of
“Stimulated Brillouin Scattering Threshold in Presence of Modulation Instability for Optical Pulse in Long Optical Fiber”, Applied Sciences, 2022 (MDPI).

## Slide 49: Laser Safety

## Slide 50: Be Careful on Web Info

## Slide 51: It Is Not Really True

## Slide 52: Conclusions
Overview on laser oscillator, amplification and MOPA system
Common optical devices
SHG and nonlinear crystals
Brillouin Instability