## Slide 1
Wavefront Aberrations
Ilaria Nardecchia INFN-Roma Tor Vergata
ilaria.nardecchia@roma2.infn.it
STGWD - Erice, 20-27 May 2026
Ettore Majorana Centre for Scientific Culture

## Slide 2
Gravitational Wave Detector Core Optics
  Cold defects: Real Mirrors vs Ideal Design
Thermal effects
  simulations
Impact of thermal effects on the ITF operation
  Interferometer simulation tool
Thermal compensation system (TCS)
  Advanced Virgo case
Next-generation wavefront actuators
ACRONYMS & REFERENCES
⚜️ Outline

## Slide 3
Substrate
  High-purity fused silica (Suprasil)
  Diameter: 35 cm, Mass: ~ 40 kg
Geometry
  Radius of Curvature (RoC): ~ 1.5 km
Manufacturing
  Substrates provided by Heraeus (Germany)
  Polished by ZYGO (USA)
  Coated by LMA (Lyon, France)
Coating
  High- and low-index amorphous oxide multilayers
  High-Reflective (HR) / Anti-Reflective
  (AR) surfaces
  Optical absorption: ~ 0.5 ppm
Credit by Maurizio Perciballi
⚜️ GW Detector Core Optics
Notes:     Ti:Ta2O5 high index material
    SiO2 for low index material

## Slide 4
Example of substrate inhomogeneities map in Advanced Virgo core optics
⚜️ Cold Defects: Real Mirrors vs Ideal Design
Example of surface figure errors map in Advanced
Virgo core optics
ΔOPL [m]
ΔOPL [m]
Real mirrors deviate from the ideal design due to residual manufacturing imperfections:
  Substrate inhomogeneities
  Surface figure errors
Consequences:
  Optical Path Length (OPL) distortions on the main YAG beam
  Deviations from the nominal RoC
Mirror quality is critical: manufacturing imperfections directly affect interferometer performance

## Slide 5
Hundreds of kW
Tens of kW
ITM
ETM
h
z axis
HR surface
AR surface
⚜️ Thermal effects
Thermal lensing
  dn/dT=9.8 x 10-6 1/K,
  Refractive index: n=1.452
  Poisson ratio: σ=0.17
  Thermal expansion coefficient: α=0.55 x 10-6 1/K
Thermo-elastic deformation of the ITM and ETM HR surfaces (⍺ ≠0)
When the ITF reaches its final working point  high circulating power  the mirror coating heats up and the absorbed heat diffuses into the substrate
FP cavity
Recycling cavities

## Slide 6
Gaussian-weighted quadratic fit:
  The interferometer is most sensitive to the central region of the mirror
  (Gaussian weights defined by the beam intensity profile, 𝑤 = beam radius)
Thermal lenses approximation:
  Thermal lenses can be treated as optical dioptres
Dp=-2.97e-05 1/m
⚜️ Thermal Lensing Simulations
ΔT[K]
T0=295 K
HR-surface
AR-surface
1) Example of FEA temperature distribution inside the ITM substrate
EXAMPLE WORKING POINT:
  Injected power ~18 W
  Absorbed power ~60 mW
Temperature map [Finite Element Analysis (FEA)]
Optical Path Length variation ΔOPL
Gaussian-weighted quadratic fit
Equivalent thermal lens
Simulation workflow:
= focal length
a = quadratic coefficient of the parabolic fit
2) OPL radial profile and Gaussian-weighted quadratic approximation

## Slide 7
⚜️ Thermo-elastic Simulations
HR-surface
RoC0=1426 m
 RoCtherm=1430 m
OPL[m]
EXAMPLE WORKING POINT:
  Injected power ~18 W
  Absorbed power ~60 mW
Temperature map [Finite Element Analysis (FEA)]
HR surface deformation [FEA]
Gaussian-weighted quadratic fit
ΔRoC
Simulation workflow:
3) Gaussian-weighted quadratic fit:
  The interferometer is most sensitive to the central region of the mirror
  (Gaussian weights defined by the beam intensity profile, 𝑤 = beam radius)
4) Spherical surface approximation:
  Thermo-elastic deformation
a = quadratic coefficient of the parabolic fit
1) Example of FEA thermo-elastic deformation on the HR-surface
HR-surface
AR-surface
2) OPL radial profile and Gaussian-weighted quadratic approximation

## Slide 8
=
+
⚜️ Thermal Lensing
Thermal lensing
Aspherical (residual)
component
Thermal lensing in the input mirrors: dominant spherical component + residual non-spherical component
Cold mirror state
Thermal lensing affects the recycling cavities and generates mode mismatch with the FP arm cavities
Spherical (quadratic)
Component
The quadratic (spherical) fit captures only the dominant focusing term

## Slide 9
⚜️ Thermo-Elastic Effect on the hr-surface
Thermo-elastic deformation on the HR-surface in the FP mirrors: dominant spherical component + residual non-spherical component
Thermo-elastic deformation
Aspherical (residual)
component
Cold mirror state
Spherical (quadratic)
component
The quadratic (spherical) fit captures only the dominant focusing term
Thermo-elastic deformation introduces wavefront distortions in the Fabry–Perot cavities
=
+

## Slide 10
⚜️Impact of thermal effects on the ITF operation
Power circulating in a generic cavity moving from the region close to the instability (g~1) toward the stable one.
TEM00
TEM01
Input beam: TEM00+TEM01
Cavity stability parameter (g) determines the filtering capability of HOMs
Thermal lensing in the ITMs causes:
  Mode mismatch with the FP cavities
  HOMs resonating in the recycling cavities
  Sideband power losses and their degradation for longitudinal/angular control
   Reduced ITF duty cyle
Thermo-elastic deformation of the HR-surfaces in all FP mirrors:
  HOMs resonating in the FP cavities
  Decrease of power circulating in the FP-cavities
  Increase of shot noise
   Sensitivity degradation at high frequency

## Slide 11
⚜️ Advanced virgo case
Optical configuration:
  Fabry-Perot arm cavities are stable (g~0.8707)
  PRC and SRC are marginally stable (g~0.9999885, very close to 1)
  PRC and SRC are extremely sensitive to deviations from the nominal optical configuration:
    Cold defects
    Thermal effects
  Even small HOM excitations can resonate inside the recyling cavities
Sideband power evolution at the interferometer bright port after reaching the final working point
After reaching the final working point, thermal effects arising in the input mirrors degrade the RF sidebands circulating in the recycling cavities
 Loss of the interferometer working point after ~20-30 minutes

## Slide 12
⚜️ Interferometer simulation tool
Full interferometer optical simulations are essential to identify the requirements for the wavefront aberration compensation
OSCAR
MAIN CAPABILITIES
  Free-space propagation of laser beams
  Simulation of optical cavities with multiple mirrors
  Analysis of mirror surface maps
  Calculation of interferometer error signals
STEADY STATE SIMULATION OUTPUTS
  Optical power distribution (carrier and sidebands)
  2D field and mode amplitudes
  Higher-order mode content
OSCAR is extensively used for thermal compensation
studies in Advanced Virgo
Developed by Jérôme Degallaix within the Virgo Collaboration
The code is publicly available on MATLAB File Exchange. (https://www.mathworks.com/matlabcentral/fileexchange/20607-oscar)
OSCAR is a
FFT optical simulation tool for gravitational-wave interferometers
EXAMPLE OUTPUTS

## Slide 13
Residual after compensation
⚜️ Thermal compensation system (TCS)
The TCS generates an aberration equal and opposite to the thermal
effect
Mirrors are suspended so they cannot be touched
The only non-contact way to heat the mirrors is via radiation
Requirements on thermal lensing and RoC variations are set by
the interferometer optical design.
  For example in Advanced Virgo:
    Thermal lensing residual < 2 nm RMS
    Radius of curvature controlled within ± 2 m
The Thermal Compensation System (TCS) compensates both cold defects and thermally induced deformations
Aberration compensation principle
The TCS introduces an opposite aberration, leaving a minimum residual

## Slide 14
+
=
Mirror heated by the YAG
Mirror heated by
TCS actuator
Cold mirror
Gaussian beam
Annular beam
⚜️ Thermal Lensing compensation strategy
+
=
Thermal lensing in the mirrors

## Slide 15
Real DAS
High-power CO₂ laser projectors are used to correct thermal lensing
CO2 wavelength (λ=10.6 µm) completely absorbed by fused silica
Heating pattern projected onto the Compensation Plates (CPs) in order to avoid injecting noise into the FP cavities
The heating profile is shaped to compensate for the distorsion
An annular beam can be generated using an axicon (conical lens)
Optimal heating pattern is achieved using a two-ring heating profile [Double Axicon System (DAS)]:
  INNER RING  thick and weak
  OUTER RING  thin and bright
⚜️ CO2 Laser Projectors
Inner ring
Outer ring
Simulated DAS
Notes: we don’t just heat the mirror — we shape the eating to match the distortion”

## Slide 16
Credit by Luciano Antonio Corubolo

## Slide 17
https://www.youtube.com/watch?v=BUUVRYy0y20

## Slide 18
⚜️ CO2 Laser Projectors: Actuation Scheme
The actuation scheme is designed to generate two independent heating patterns
Central Heating (CH)
  Mimics the YAG thermal lens
  Used to mitigate thermal transients during loss of lock
Double Axicon System (DAS)
Compensates thermal lensing due to uniform coating absorption
Notes: These actuation schemes enable tailored and tunable heating patterns on the CPs

## Slide 19
⚜️ CO2 Laser Projectors in Advanced Virgo
Installation in acoustic enclosure
CO2 laser ON
CO2 bench
Experimental implementation in Advanced Virgo

## Slide 20
⚜️ Thermo-Elastic Effect on the hr-surface
Thermo-elastic deformation on the HR-surface in the FP mirrors: dominant spherical component + residual non-spherical component
Thermo-elastic deformation
Aspherical (residual)
component
Cold mirror
Spherical (quadratic)
component
=
+
Ring heaters compensate the quadratic component
+
+
=
HR-surface deformation after RH

## Slide 21
⚜️ Thermo-Elastic Effect on the hr-surface
Thermo-elastic deformation on the HR-surface in the FP mirrors: dominant spherical component + residual non-spherical component
Thermo-elastic deformation
Aspherical (residual)
component
Cold mirror
Spherical (quadratic)
component
=
+
Ring heaters compensate the quadratic component
+
+
=
HR-surface deformation after RH

## Slide 22
AR-surface
⚜️ Ring Heater RADIATIVE PROJECTOR
Radiative actuator used to compensate thermo-elastic RoC variations.
The RH is a resistive heater installed around each mirror to heat the periphery of the optics.
Main components:
  2 Pyrex Glass rings
  NiCr conductive wire
  Copper shield
Adavanced Virgo RH
Top view
3D view

## Slide 23
⚜️ Ring Heater Simulations
AR-surface
HR-surface
T0=295 K
OPL[m]
HR-surface
AR-surface
RH-induced thermo-elastic deformation decreases the mirror RoC
Simulation workflow:
Temperature map [FEA]
HR surface deformation [FEA]
Gaussian-weighted quadratic fit
ΔRoC
1) Temperature distribution inside the ITM substrate for RH power 𝑃=7W
HR-surface
2) Thermoelastic mirror deformation
Compensation is almost purely spherical (>98%)
3) Gaussian-weighted quadratic fit
Typical RoC dynamics: ~ -2 m/W

## Slide 24
Alumina ceramic heater
⚜️ CHRoCC RADIATIVE PROJECTOR
CHRoCC: Central Heating Radius of Curvature Correction (Developed by EGO group)
Radiative actuator complementary to the RH increases mirror RoC (same effect as YAG heating)
Radiative element: black-body emitter + elliptical reflector
OPTICAL SIMULATION
FEA SIMULATIONS
1) Temperature distribution inside the ITM substrate for CHRoCC power 𝑃=17W
2) Thermoelastic mirror deformation
Compensation is almost purely spherical

## Slide 25
*Developed by LIGO Group of the University of Adelaide (Australia)
ITM
SLED
ON-AXIS SET UP
HWS
Telescope of magnification
M
PROBE BEAM
L
Δxi
W
W’
CCD
HWS plate
OFF-AXIS SET UP
⚜️ Hartmann-Wavefront Sensor (HWS)
HWS
Telescope of magnification
M
TM
Measures wavefront variations relative to a reference wavefront
Uses an uncoherent probe beam [fiber coupled super luminiscent diode (SLED)]
In the image plane of the aberrated surface
HWSs are used in two different configurations:
  ON-AXIS
  OFF-AXIS
RoC relation:
RoCTM= M2 RoCHWS

## Slide 26
ITF locked at 25 W without TCS:
 positive curvature;​
After engaging DAS:
 curvature goes to zero;​
ITF unlocked with DAS ON:
 negative curvature appears
ITF relocked with DAS ON:
 curvature equal to zero.
⚜️ HWS-ON AXIS
Example of absorption measurements in the input test mass of Advanced Virgo
Central heating actuation overimposed on the RH one
They are fundamental for the TCS pre-commissioning:
  to align the CO2 actuators on the CPs
  to evaluate the absorption values in the test masses
  to characterize all thermal actuators
Real-time monitoring of thermal curvature evolution

## Slide 27
TM
M1
M2
M3
TM
Tower
ITF BEAM
⚜️ HWS-OFF AXIS
Credit by Maurizio Perciballi
Probe beam injected off-axis with respect to the ITF beam
Sensitive to the HR-surface thermo-elastic deformation

## Slide 28
Carrier field on the
Dark Fringe with the ITF in the final working point
⚜️ Phase Cameras (PC)
The phase camera (PC) senses aberrations in the beam propagating through the interferometer
Two phase cameras are installed at the bright and dark ports of the interferometer
Heterodyne detection allows independent measurement of the carrier, upper sideband, and lower sideband
Example measurement

## Slide 29
⚜️ Advanced Virgo TCS
HWS OFF-AXIS
HWS ON-AXIS
PRC
SRC

## Slide 30
⚜️ Point Absorbers (PA)
Localized high-absorption regions on the HR mirror surfaces:
  small
  randomly distributed across the optics
  characterized by optical absorption much higher than the average coating absorption
  Possible origins:
    coating defects (spectroscopic analyses revealed high concentrations of aluminium in several absorbers)
    dust particles deposited during installation or handling
  First identified in LIGO ITFs and later observed in Virgo as the circulating power increased
Effects on the mirror:
  Localized thermo-elastic deformation of the HR surface
  Localized thermal lensing in the substrate
Effects on the interferometer:
  Generation of HOMs in both the FP and recycling cavities
  Reduction of the circulating power in both the FP and recycling cavities
  Degradation of the interferometer duty cycle and sensitivity
[Aidan F. Brooks, et al.. Appl.
Opt. 60, 4047-4063 (2021)]
Examples of PA on LIGO mirrors observed under a microscope
Point absorbers on AdV mirrors observed with a thermal camera and the HWS

## Slide 31
⚜️ Point Absorbers compensation
The correction strategy aims at reducing the thermal gradient induced by the point absorbers by heating the surrounding colder areas
The correction principle is based on reproducing a target thermal deformation using a binary heating mask.
Each square in the mask acts as an independent thermal actuator that can be either ON or OFF.
The optimal mask pattern is reconstructed through the influence matrix formalism.

## Slide 32
⚜️ Point Absorbers actuator
Radiative actuator conceptually similar to CHRoCC
Radiative element:
  black-body emitter
  parabolic reflector
The thermal pattern is first generated at the object plane and then imaged onto the test mass
Installed in air outside the vacuum system
The thermal radiation enters the tower through a ZnSe viewport
1: Parabolic reflector and ceramic heater
2: Focusing Germanium Lens
3: Binary mask
4-6: Steering mirrors
5: Imaging Germanium Lens (8")
7: ZnSe viewport
8: Test Mass
OPTICAL SIMULATION
Experimental patterns

## Slide 33
⚜️ IPATSiA: Point Absorber simulator
IPATSiA (Infrared Point Absorber Thermal Simulator Actuator)
CO2 laser system used to generate artificial localized thermal defects on the HR surface of the mirror
Dynamic control of the artificial point absorber:
  Position on the mirror surface
  Size
  Injected power
Developed to study the interferometer response to localized defects
IPATSiA further confirmed that HOMs generated by localized defects introduce additional noise in the Advanced Virgo sensitivity
IPATSiA experimental setup
Optical layout
CO2 beam projected on the mirror

## Slide 34
⚜️ Next-generation wavefront actuators
Thermal effects previously considered negligible will become increasingly critical
  Current thermal actuators produce only axisymmetric compensation patterns. Only the spherical part of the thermo-elastic deformation on the HR-surface
  is componsated
  Localized defects generate non-axisymmetric and not-spherical aberrations
  (cold defects, DAS imperfections)
  Aspherical residual thermo-elastic deformation increases with the circulating
  power
Example of complex residual deformation (non-axisymmetric)
A new generation of thermal actuators is being developed to address the MW-level circulating powers expected in future GW detectors such as Einstein Telescope.

## Slide 35
⚜️ DEFORMABLE MIRROR (DM)
.
Goal
Use a deformable mirror coupled to the CO₂ laser to compensate
localized defects by projecting complex non-axisymmetric heating
patterns onto the CPs.
Method
DM shapes the phase of the CO2 beam producing
the required intensity pattern on the CP
Long-standing expertise on deformable mirrors at Tor Vergata since 2016.
  Latest deformable mirror tested: DM192-15 (by ALPAO, 192 magnetic actuators with a grid layout)

## Slide 36
⚜️ DEFORMABLE MIRROR (DM)
The Modified Gerchberg–Saxton algorithm iteratively retrieves the phase map that must be applied by the deformable mirror in order to reproduce a desired intensity distribution.
Experimented tests ongoing in Tor Vergata Lab

## Slide 37
⚜️ FROnt Surface Type Irradiator (FROSTI)
Residual aspherical thermo-elastic deformation increases with circulating power
Residual aspheric deformation becomes limiting above 𝑃_𝑐𝑎𝑣∼0.5–0.7 MW (VIR-0497D-22, LIGO-G2400546)
LIGO developed a correction scheme based on an RH-like reflector
An optimized profile projects the heating pattern directly onto the HR surface (FROSTI, DCC-G2402386)
Gray-body radiation reshaped into an annular thermal pattern
FROSTI prototype assembled and tested at LIGO
.
Notes: the two “front” (facing the test mass) and “back” reflector sections, which are joined to form an annular nonimaging elliptical trough. The inset displays one of the
eight heater elements, which are placed along the reflector circumference

## Slide 38
⚜️ Take Away message
Thermal effects are a major limitation for high-power GW interferometers.
The Thermal Compensation System has proven to be fundamental for the operation of gravitational-wave interferometers, especially for Advanced Virgo, where the recycling cavities operate in a marginally stable configuration.
Traditional TCS compensates mainly for first-order axisymmetric aberrations.
At MW-level circulating powers, non-axisymmetric and higher-order aberrations are becoming increasingly critical.
Thermal compensation is evolving toward adaptive correction
of complex optical aberrations.
 New adaptive thermal actuators are under development for next-
generation of GW detectors.

## Slide 39
~ THANK YOU ~

## Slide 40
RoC | Radius of Curvature
FP | Fabry-Pèrot
PRM | Power Recycling Mirror
PRC | Power Recycling Cavity
CP | Conpensation Plate
ITM | Input Test Mass
OPL | Optical Path length
DP | Dark Port
RH | Ring Heater
HWS | Hartmann Wavefront Sensor
PC | Phase Camera
DAS | Double Axicon System
CH | Central Heating
SLED | Superluminiscent Light Emitting Diode
DAS IN | DAS inner ring
DAS OUT | DAS outer ring
HOM | Higher Order Modes
CHRoCC DM PA | Central Heating Radius of Curvature Correction Deformable mirror Point Absorber
⚜️ ACRONYMS

## Slide 41
⚜️ REFERENCES
.
[1] R. Lawrence et al., Adaptive thermal compensation of test masses in Advanced LIGO, Class. Quantum Grav. 19, 1803 (2003)
[2] The Virgo Collaboration, Advanced Virgo Baseline Design, Virgo internal note VIR-0027A-09, (2009).
[3] H. Luek et al., Thermal correction of the radii of curvature of the mirrors for GEO600, Class. Quantum Grav. 21, S985 (2004)
[4] Central heating radius of curvature correction (CHRoCC) for use in large scale gravitational wave
interferometers, CQG, 30(5):055017, 2013
[5] Brooks A., Hartmann Wavefront Sensors for Advanced Gravitational Wave Interferometers, Ph.D. thesis, University of
Adelaide, (2007) [6] A. Rocchi et al., Thermal effects and their compensation in Advanced Virgo, J. Phys.: Conf. Ser. 363, 012016 (2012)
[7] I. Nardecchia, Control of optical aberrations in advanced gravitational wave detectors, PhD Thesis, 2016.
[8] L. van der Schaaf, K. Agatsuma, M. van Beuzekom, M. Gebeyehu, J. van der Brand, Advanced Virgo phase cameras, J. Phys.:
Conf. Ser. 718 072008 (2016)
[9] David Voelz,Computational Fourier Optics, SPIE press